## Slide 1: Preliminary Experimental Results and Experimental Methods for Mercury Contaminated OPC Testing: EPA Methods 1313 and 1315
Laira Kelley, Andrew C. Garrabrants, Rossane DeLapp, David S. Kosson
Vanderbilt University
Nashville, Tennessee, USA
November 3rd, 2021

## Slide 2: Project Goal and Objectives
Goal: Propose and conduct experimentation for testing of mercury-impacted OPC materials using Method 1313 and Method 1315.
  Objective 1: To outline the findings of method development testing, giving guidance to what preservation methods need to be used, as well as filtration techniques and preparation and storage of samples throughout experimentation.
  Objective 2: To outline the methodology for Method 1313 and Method 1315 so that procedures reflect the findings of preliminary testing and are adapted to address the preservation of mercury-contaminated material.

## Slide 3: Behavior of Mercury
Elemental Mercury (Hg(0))
    Liquid at room temperature
    Vapor Pressure of 0.17 Pa at 20°C
    Solubility of 60 µg/L in water
    Easily volatilized
Forms amalgams with other metals, salts, and organic compounds
Compounds of interest include HgCl2 and HgS
    HgCl2 solubility of 69 g/L (very soluble in water)
    HgS solubility of 2E-53 g/L
Hg solid phases in contact with aqueous solution with Cl- and SO42- (10-3 mol/kg; 1 bar)

## Slide 4: Material Compatibility
Interactions with HDPE, LDPE, Nylon, and Polypropylene
  Linked to mercury sorption from low-level solutions (<1 mg/L)
  Reported losses of up to 43% in HDPE digitubes (Zhang, 2020)
  LDPE bags reported concentration of Hg 15% lower than that stored in glass container (Liescheski, 1999)
  Nylon is utilized as a sorbent for mercury (Dunham-Cheatham, 2020)
PTFE and Glass Containment
  Mercury solutions of 0.003-0.013 µg/L are stable in both PTFE and glass over 13 day period when preserved with HCl (Guevara, 2013)
  Use of preservation for samples with glass containment reports no significant losses over several weeks (Zhang, 2020)
HDPE, polypropylene, and nylon should be avoided and replaced with glass or PTFE materials wherever possible.

## Slide 5: Stability of Low-Level Mercury Solution in Time-Dependent Leaching Test Eluate
Objective
  Quantify losses of mercury from low-level mercury standard stored in borosilicate glass vials with PTFE lid liners over 2-week hold time for Methods 1313 & 1315 (no preservation).
Approach
  50 µg/L mercury solution, pH adjusted to ~11
  Stored at room temperature
  Sampled at 1 week and 2 week
Results
  Minimal losses occur in low-level solutions when PTFE and glass are storage materials
  % Difference to Standard: 0.6%

## Slide 6: Losses of Dissolved Mercury During Filtration of Aqueous Samples
Objective
  To evaluate the potential for sorption losses from low-level mercury solutions due to contact with polypropylene housing of PTFE filtration cartridges.
Approach
  50 µg/L mercury solution pH adjusted to: ~ 2, 5, 7, 9, 11
  Filtered 10-mL aliquots of each pH through glass syringe and PTFE filter cartridges
  Unfiltered sample of each pH value
Results
  Losses to filtration cartridge occur at a pH>9.0
  % Diff to standard for pH 11: 7.6%
  % Diff to standard for all other pH: <1.0%

## Slide 7: Potential Sorption of Mercury to Milling Media
Objective
  To determine if mercury sorption occurs when using magnesium stabilized zirconium milling media and low-level mercury solution.
Approach
  50 µg/L mercury solution adjusted to pH ~11
  Added one milling ball to solution, 3 replicates and control
  Sampled at 30 min, 1 hour, 2 hours
Results
  Minimal sorption of aqueous mercury occurs over prolonged contact period
  % Diff to Standard: <0.5%

## Slide 8: Potential Sorption of Elemental Mercury to Milling Media
Objective
  Determine if mercury sorption occurs when using magnesium stabilized zirconium milling media and liquid elemental mercury.
Approach
  2 mm height of elemental mercury in glass vial
  Milling ball added to vial, no replicates
  Rinse ball with DI water after 1 hour of contact
  Back Extract milling ball in 2% HCl for 48 hours, 3 repetitions
Results
  Sorption occurs, 0.64 mg/L removed from first 48 hour HCl soak
  mercury removed from milling surface with HCl soak
Chart: Extract Position
| 0
initial rinse | 20
back extract 1 | 640
back extract 2 | 80
back extract 3 | 50

## Slide 9: Sample Casting & Method 1315 Testing
Materials for Casting
  Cast solid material into specially fabricated PTFE molds fitted with a leaching attachment for EPA Method 1315 1-Dimensional testing
    Molds allow for 5-cm diameter by 10-cm length cylinder to be cast, sealed, and cured all within same PTFE containment
  Cast flat sheets in PTFE bags for crushing of material for EPA Method 1313 Testing

## Slide 10: Solid Sample Preparation to Minimize Losses
Casting of Doped OPC
  Use stand mixer fitted with glass bowl, specially coated PTFE beater, and PTFE shield to minimize air exposure
  Low speed blending of OPC with reagent water followed by direct mercury addition in final minutes of blending

## Slide 11: Solid Sample Preparation
HgCl2 Mix:
40 mg Hg /kg material
Blend OPC and water, directly pipette HgCl2 into mix during last minute of blending
Pour into cylindrical molds and PTFE bags, seal and cure
Hg(0) Mix:
40 mg Hg /kg material
Blend OPC and water, pour into cylindrical molds and allow to set for 30 minutes
Directly inject Hg(0) using micropipettes 1.3 cm into the center of each cylinder, then seal and cure
Cast undoped PTFE bags for baseline 1313 testing

## Slide 12: Sample Handling to Minimize Losses
Crushing Material
  Planetary ball mill outfitted with magnesium stabilized zirconium milling media
Filtration
  For pH < 9.0, use glass syringes with PTFE filter cartridges
  For pH > 9.0, centrifuge and decant samples
Appropriate Vessels for Storage
  Glass vials fitted with PTFE or PCTFE lid liners
  PTFE bottles or bags

## Slide 13: Mercury Sample Characterization
Liquid samples - preparation
  1% nitric acid sample matrix (Christmann, 1976)
  Gold addition at 200 µg/L for stabilization
    Added to both calibration standards and samples
Liquid samples - analytical
  Inductively coupled plasma mass spectrometer (ICP-MS)
    EPA Method 6020B
    22 ng/L (ppt) detection limit for Hg0
  Inductively coupled plasma optical emission spectrometer (ICP-OES)
    EPA Method 6010D
    10 µg/L (ppb) detection limit for Hg0
Solid samples
  Mercury analyzer with integrated balance
    Typical samples have particle size ≤ 2 mm
    EPA Method 7473
    1 ng/g (ppb) detection limit for Hg0

## Slide 14: Next Steps
Continue Method 1315 with HgCl2 OPC samples
Complete sample prep for HgCl2 OPC, and complete Method 1313
Begin Method 1315 with Hg(0) samples after curing is complete
Complete baseline Method 1313 with undoped OPC for use in modeling of Hg(0)